## Slide 1: 熱プラズマを用いた 材料プロセッシング における計測技術
第18回若手科学者によるプラズマ研究会
2015年3月4日
新しい工業プロセス
熱プラズマ発生システム
電極現象の観測
放電現象の観測
インフライト粒子の観測
九州大学
渡辺隆行

## Slide 2: 新しい 工業プロセス
プラズマを用いた革新的ガラス溶融プロセスは洞爺湖サミット(2008年)で紹介されました
第18回若手科学者によるプラズマ研究会
2015年3月4日

## Slide 3: 150年間に改革がないガラス製造
CO2, H2O, SO2
ガラス原料
3 – 5日間
成形
工程
15 - 30m
5 - 11m
均質化と気泡の除去に長時間の加熱が必要
エネルギー多消費プロセス

## Slide 4: プラズマによる革新的ガラス溶融プロセス
溶融時間の大幅な短縮
粒子単位での均一なガラス製造
珪砂の塊状化を抑制
インフライト中に分解ガスを除去
必要エネルギーは1/3

## Slide 5: プラズマによる革新的ガラス溶融プロセス
72SiO2-16Na2O-10CaO-2Al2O3-0.5SO3
SiO2-Na3CO3-CaCO3-Al2O3-Na2SO4
原料
製品
ソーダ石灰ガラス
原料の造粒粉体
溶融ガラス粒子
60mm
ガラス製品
Si
Ca
Si
Ca

## Slide 6: プラズマによる革新的ガラス溶融プロセス
Multi-Phase
Arc
Oxygen Burner
Granular Raw Materials
Gas Outlet
~5m
Refining
Furnace
Melting
Furnace
Glass
Melt
Glass Melt
Oxygen Burner
Stirring
Granular Raw
Materials
High-Speed
Refining
Melting
Furnace
Refining
Furnace
Multi-Phase
Arc
多相交流アークで大型プロセスを実現できる

## Slide 7: 従来の熱プラズマシステムは産業的に対応できない
従来の熱プラズマ発生方法を改善
直流放電，交流放電，高周波放電
高効率化
大面積化
高温場の制御（時間的，空間的）
反応性ガスの利用による高活性化

## Slide 8: 多相交流アーク

## Slide 9: アーク放電は電極の観測がむずかしい
直流放電アークの電極を「見たい」
しかし，高輝度のアークが邪魔
バンドパスフィルター
レーザーストロボ
電極だけを「見る」技術の開発
交流放電アークはもっと複雑

## Slide 10: 電極現象観測のための高速度カメラシステム
Measurement
Oscilloscope : Scope Corder (Yokogawa)
Sampling frequency : 107 Hz
High-speed camera measurements
FASTCAM SA5 (Photron Inc.)
Frame rate: 5.0×103 fps
Exposure time:
18 µs (for electrode measurements)
200 µs (for tungsten vapor observations)
Temperature measurements (Upper view)
Band pass filter: 785±2.5 nm, 880±5 nm
Tungsten vapor observations (Side view)
Band pass filter: 393±0.5 nm, 738±1.5 nm
Power (Arc current: 100 A for each electrode)
12-phase arc: 25 kW
Shield gas (Ar) ：2, 5 L/min for an electrode
Plasma conditions

## Slide 11: 電極現象観測のための高速度カメラシステム
785 nm
880 nm
Free of line emission from plasma at 785nm, 880nm.
Two band pass filters were selected at 785nm (FWHM: 10 nm), 880nm (FWHM: 5 nm).

## Slide 12: 電極現象観測のための高速度カメラシステム
灰色体に対する
プランクの法則
Filter
785 nm
Filter
880 nm
W/Ar
Filter
393 nm
W I
Filter
738 nm
Ar I
電極温度

## Slide 13: 多相交流アークの電極現象
Herts-Kundsen Equation
Mass flux of vapor
Electrode temperature
Mass of the atom
Saturation vapor pressure
at temperature TC
Boltzmann constant
Evaporation rate
Surface area
at temperature TC
Escape factor
~1 at anodic period
M. Boselli et al J Phys D: Appl Phys
46 (2013) 224006
~10-2 at cathodic period
V. Nemchinsky J Phys D: Appl Phys
45 (2012) 135201
Evaporation Rate:

## Slide 14: 多相交流アークの電極現象
Evaporation Rate of W Electrode during AC Cycle
Electrode mainly evaporated only at anodic period
Higher surface temperature due to larger heat transfer
Direction of electric field
Evaluated evaporation rate was evaluated as 3 mg/min

## Slide 15: 多相交流アークの電極現象
Total number of droplet ejection
Anodic period, Cathodic period
Transition from cathodic to anodic period
Number of large droplet ejection
Cathodic period
Transition from cathodic to anodic period
Anodic period
Cathodic period
0
10
20
30
40
50
Droplet Volume [10
-14
m
3
]
Phase
(n-1)
p
(n-1/2)
p
n
p
(n+1/2)
p
(n+1)
p
Droplet ejection
(Large)
Droplet ejection
(Total)
0
50
100
150
200
0
1
2
3
Number of Droplet [-]
Number of Droplet
above 250
m
in Diameter [-]
Phase
(n-1)
p
(n-1/2)
p
n
p
(n+1/2)
p
(n+1)
p
Anodic period
Cathodic
period

## Slide 16: 多相交流アークの放電現象
Snapshot
Binary Image
Temporal Characteristics
Spatial Characteristics
Convert the BMP file to CSV document
Convert the CSV to binary (black-white) image by setting luminance value
Record the discharge behavior
Select the video images at pixel of 768×766 and saved to bitmaps at interval time of 0.1 ms
Calculate the luminance area according to the pixel scale to obtain the time fluctuation of arc luminance area (mm2)
Accumulate the binary images and average into contour map to obtain the arc existence area
Frame rate: 105 frames/s
Shutter speed: 0.37 µs

## Slide 17: 多相交流アークの放電現象
Arc fluctuation amplitude of CW pattern is high.
Complex arc discharge behavior.
A number of alternative paths leads to large variation of arc luminance area.
Arc fluctuation amplitude of FF pattern is low.
Arc length is regular and similar.
Well-defined conducting path between intervals or nearby electrodes.
CW pattern
FF pattern

## Slide 18: 多相交流アークの放電現象
CW pattern has specific frequency of 100 Hz in the central area, originated from the periodical arc path through the center.
CW pattern
CW pattern
FF pattern

## Slide 19: インフライト粒子の計測
第18回若手科学者によるプラズマ研究会
2015年3月4日
Does commercial system indicate real particle temperature?

## Slide 20: インフライト粒子の温度計測
Temperature measurement by DPV-2000
PD-1 787±25nm
Central 400µm fiber
Dichroic Mirror
F1
F2
PD-2 995±25nm
Planck’s law
Gray Body Assumption
Same Emissivity at λ1 and λ2.
Two-Color Radiation

## Slide 21: インフライト粒子の温度計測
Calibration is required for particle temperature measurements.
Before calibration
After calibration

## Slide 22: インフライト粒子の温度計測
250×100 pixels = 8.5×3.5 mm
785±2.5 nm
880±5.0 nm
High-speed images of in-flight particles at different wavelengths
Schematic images of particle measurement by HSVC

## Slide 23: インフライト粒子の温度計測
CW pattern
CW pattern
Fluctuation of Arc
Fluctuation of Particle Temperature
FF pattern
FF pattern
Higher fluctuation of arc luminance area caused larger dispersion of particle surface temperature.
Higher temperature can be obtained in CW pattern due to the particles can be directly heated by arc passing through the center.

## Slide 24: インフライト粒子の温度計測
FF pattern
CW pattern
FFT of Arc Luminance Area
FFT of Particle Temperature
CW pattern
FF pattern
The particle temperature reflects the same periodic fluctuation with arc in CW pattern, while there is no significant periodic signal in FF pattern.
 CW pattern has specific frequency of 100 Hz in the
central area, originated from the periodical arc path
through the center.

## Slide 25: まとめ
廃棄物処理
マテリアルプロセス
ナノテクノロジー
バイオプロセス
エネルギーシステム
熱プラズマ
プロセッシング
熱プラズマは単に「高温熱源」として用いられてきた。
熱プラズマを「化学的に活性なプラズマ」として考える。
環境問題の解決
高効率・高速物質処理
高効率・高速物質変換
工業プロセスの実現
プラズマプロセスの開発における世界への情報発信基地を目指す。
大気圧プラズマ中の電子，原子，分子の反応過程を解明することによって，新しい材料合成プロセス，廃棄物処理プロセスを開発する。